PS

www.kau.edu.sa/src

COVER PAGE

Final Report

Name of College: Engineering

Name of Department: Chemical and Materials Engineering Department

Title of Research : “Production of Sodium Aluminate From Local Clays”

Final Report for Project NO: (107/425 )

Duration of the project for which the report is written : 10 months

Names of the Investigator (s) :

-Principal Investigator: Prof. Dr. AbdulRahim Ahmad Al-Zahrani

-Co-Investigator: Prof. Dr. Mohammed H. Abdel-Majeed

-Co-Investigator:

-Co-Investigator:

-Co-Investigator:

Date of Submission of this report : H 1425 / 1 / 11

ملخص تقرير نهائي  ( عربي )

1- عنوان البحث : انتاج الومينات الصوديوم من خامات الطفله السعوديه

2 – الباحث الرئيسي : أ.د. عبدالرحيم أحمدعمر الزهراني

الهندسه 3- أسم الكلية :

4- أسم القسم : الهندسه الكيميائيه وهندسة المواد

### الملخص لا يتم أنتاج الومينات الصوديوم محليا وأنما يتم توفير أحتياجات الصناعة المحلية من هدة المادة عن طريق الأستيراد من الخارج. ويعتبر خام البوكسيت الدي يحتوي علي 40 – 60% الومينا وما لا يزيد عن 7% سيلكا المصد ر الرئيسي لأ نتاج الومينات الصوديوم . وهدا الخام يتوفر في أراضي المملكة بكميات محدودة جدا. ويهدف البحث الي دراسة أمكانية أنتاج الومينات الصوديوم محليا لتلبية أحتياجات الصناعة الوطنية من المروبات وللأ ستخدامات الأ خري باستخدام خامات الطفلة الوطنية المتواجده في أراضي المملكة بدلا من خام البوكسيت قليل التواجد محليا ود لك بطريقة الكلسنة مع الجير. وقد تم تنشيط طفلة كاولين وطني تحتوي علي 4و29% اكسيد الومنيوم بتسخينة عند درجة 700 مئوية لمدة ساعة واحدة وتم بعد دلك تحميص الكاولين مع كربونات الكالسيوم ثم معالجة ناتج التحميص بمحلول كربونات الصود يوم لأ ستخلأ ص الا لومينا الموجودة في الطفلة علي صورة الومينات الصوديوم. وقد تم في خطوة التحميص دراسة تأ ثير العوامل التالية علي استخلاص الا لومينا من طفلة الكاولين الوطنية : درجة حرارة التحميص من 1200 الي 1400 درجة مئوية - زمن التحميص من نصف الي ثلا ث ساعات – والنسبة الجزيئة لأ كسيد الكالسيوم الي مجموع اكسيدي الا لومنيوم والسيلكون من 5و2 الي 0و4 ودلك تحت ظروف أستخلاص ثابتة تساوي درجة حرارة 70 مئوية وزمن نصف ساعة ونسبة جزيئية من اكسيد الصوديوم الي اكسيد الا لومنيوم تساوي 2و2 . وقد بينت نتائج الدراسة المعملية أن أستخلاص الالومينا يزداد بزيادة درجة الكلسنة في المدي من 1250 الي 1350 درجة مئوية ثم تقل بزيادة درجة الكلسنة الي 1400 درجة مئوية. كما بينت نتائج الدراسة أن تأثير زمن الكلسنة علي درجة استخلا ص الالومينا من الطفلة يعتمد علي كلا من درجة حرارة الكلسنة والنسبة الجزيئية لأ كسيد الكالسيوم الي مجموع اكسيدي الا لومنيوم والسيلكون. وكدلك وضحت الدراسة أنة بزيادة النسبة الجزيئية لأكسيد الكالسيوم الي مجموع اكسيدي الا لومنيوم والسيلكون فأن الأ ستخلاص يزداد بزيادة درجة حرارة التحميص الي 1300 درجة مئوية وأن هدا التأ ثير يعتمد علي كلا من درجة حرارة وزمن الكلسنة. وقد تمت التوصية بأ ستخدام ظروف تحميص 1350 درجة مئوية وزمن ساعة لكلا من درجة حرارة وزمن التحميص ونسبة جزيئية لآ كسيد الكالسيوم الي مجموع اكسيدي الا لومنيوم والسيلكون تساوي 5 و2 حيث كانت درجة أستخلا ص الا لومينا من الطفلة تساوي 23و48 % تحت هدة الظروف , وبالنسبة لخطوة الأ ستخلا ص بمحلول كربونات الصود يوم فقد بينت نتائج الدراسة تأ ثير صغير نسبيا لكلا من درجة حرارة وزمن الأ ستخلا ص وأيضا للنسبة الجزيئية لأ كسيد الصوديوم الي اكسيد الالومنيوم علي درجة أستخلا ص الالومينا من الطفلة حيث كانت أ قصي درجة أستخلا ص للالومينا من طفلة الكاولين المحلية تساوي 55% عنذ ظروف 90 مئوية لدرجة الحرارة و 3 ساعات لزمن الأ ستخلا ص ونسبة جزيئية لأ كسيد الصوديوم الي اكسيد الا لومنيوم تساوي 0و3 . وتبين نتائج الدراسة الأ نخفاض النسبي لأ ستخلا ص الا لومينا علي صورة الومينات الصوديوم من خام طفلة الكاولين الوطني بأ ستخدام طريقة الكلسنة بالجير وتوصي بدراسة مدي مناسبة طريقة الكلسنة مع الجير والصودا بديلا عن طريقة الكلسنة مع الجير فقط لأنتاج الومينات الصوديوم من طفلة الكاولين الوطنية.

www.kaau.edu.sa/src

FINAL SUMMARY (English)

- Title of Project: Utilization of Saudi Clays in Bleaching of Edible Oils

2 Principal Investigator: Dr. AbdulRahim Ahmad Omar Al-Zahrani

3. Name of the College: Engineering

4. Name of the Department: Chemical and Materials Engineering Department

SUMMARY Sodium aluminate is not produced locally in the Kingdom. It is imported to satisfy local industry requirements and for other applications. The principal source for manufacture of sodium aluminate is bauxite ore, a mineral containing about 40-60% alumina and less than 7% silica. Limited reserves of bauxite have been discovered in the Kingdom's land. This study was carried out to investigate the possible manufacture of sodium aluminate to satisfy local demands from local Saudi clays that are extremely abundant in the Kingdom' land, rather from the much scarcer bauxite, using the lime sinter process. Local kaolinitic clay containing 29.4% Al2O3 was activated by calcination at 700oC for one hour, the activated clay was then sintered with calcium carbonate, followed by leaching the sintered mass with sodium carbonate solution to solubilize alumina in the clay as sodium aluminate. In the sintering step, the effect of the following parameters on alumina extraction was investigated, sintering temperature, from 1200 - 1400oC , duration of sintering, from 0.5 - 3.0 hour, and mole ratio of CaO / Al2O3 + SiO2, from 2.5 - 4.0, and fixed leaching conditions of 70oC, 0.5 hour and 2.2 for temperature, period of leaching and Na2O / Al2O3 mole ratio respectively. The results obtained from the bench scale experiments indicate an increase in alumina extraction at a temperature range of 1250 – 1350oC, followed by a decrease with increasing temperature to 1400oC. The effect of period of sintering on alumina extraction from local clay is found to depend on both sintering temperature and the mole ratio CaO / Al2O3 SiO2 used. The results obtained indicate that as the mole ratio CaO / Al2O3 + SiO2 increases , the recovery of alumina from local clay increases up to a sintering temperature of 1300oC. This effect is more pronounced by increasing both temperature and period of sintering. The recommended conditions for the sintering step are: 1350oC, one hour and 2.5 for sintering temperature, sintering period and CaO / Al2O3 + SiO2 mole ratio, respectively. The percent alumina extraction under these conditions is 48.32. The results obtained from the leaching step indicate relatively slight effect for increasing leaching temperature, leaching period and Na2O / Al2O3 mole ratio on alumina extraction. The maximum alumina extraction from local clay achieved is 55% at leaching conditions of 90oC, 3.0 hour, and 3.0 for leaching temperatures, leaching period and Na2O / Al2O3 mole ratio, respectively. These relatively low results suggest evaluation of other processes such as the lime-soda sinter process for production of sodium aluminate from local clay rather than the lime sinter process.